DLB Series

Overview

The DLB Series is a polypropylene metallized film

with solvent resistant plastic case filled with resin

sealing (UL 94 V-0)

Application:

The DLB series is designed for DC-link applications.

For compact design of: Frequency converters.

Industrial and high-end power supplies.

Solar inverters.

Benefits

High capacitance density, compact.

Excellent self-healing properties.

Overvoltage capability.

Low losses with high current capability.

High reliability.

Long useful life.

RoHS-compatible.

Construction

Dielectric: Polypropylene (PP) film.

Protection: Solvent resistant plastic case with resin sealing (UL 94 V-0)

Terminals: Parallel wire leads, lead-free tinned

2-pin and 4-pin versions

Standard lead lengths: 6 ±1 mm

Special lead lengths are available on request

Structure of ordering code

DLB - 1100 - 30 - P2  0

1    2    3  4   5

1  Series code

2  Rated voltage: 1100 V

3  Rated capacitance: 30 μF

4  Designs Type

5  Internal use

DLB Series

Electrical data

Reference standards                         IEC 61071 , IEC 60068 , RoHS compliance.

Rated capacitance (CN)                       4.5μF ... 90μF

Rated voltage (UNDC)                         800V ... 1300V

Standard capacitance tolerance                 K: ±10% , J: ±5%

Dissipation factor tan δ (100Hz@20°C)           ≤ 10×10-4

Test voltage between terminals UTT              1.5 UNDC , 10s

Test voltage between terminals and case UTC      3000 VAC, 10s

Insulation Resistance                        Ri x C ≥ 10,000s at 100 VDC/1min at +25°C

Operating temperature range (case)             –40 °C ... +105°C

Max. permissible ambient temperature           +85°C, operation at rated power, rated current

and natural cooling

Storage temperature Θstg                    –40 ... +105 °C

Climatic category                            40/85/56

Damp heat test      - Test conditions          Temperature : +40 °C

Relative humidity : 93% ±2%

Test duration : 56 days

- Performances           Capacitance change : ≤ ± 5%

tgδ change: ≤50% of nominal value at 1 kHz

Insulation resistance: ≤50% of limit value

Expected lifetime                           100 000 h at UNDC @ Θhs 70°C

Fit rate                                   50 (100 000 h at Θhs 70°C)

Resistance to soldering heat

-Test conditions:        Solder bath temperature= +260±5°C dipping

time (with heat screen) ≤4s

-Performance:          Capacitance change: ≤ ±1%

tgδ change : ≤0,0010 at 1kHz

Visual inspection No visible damage

DESIGNS

2-pin version                                        4-pin version

Designs P2                                      Designs P4

DLB Series

UNDC  1300V @ Θhs 70°C      1100V @ Θhs 85°C

| Ordering code | Cn (μF) | DIMENSIONS (mm) |  |  |  |  | Imax 10kHz@60° (A) | Imax 20kHz@60° (A) | Rs (mΩ) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | L | B | H | P | P1 |  |  |  |
| DLB-1300-4.5-P20 | 4.5 | 42 | 17 | 28 | 37.5 | - | 6 | 6 | 16.1 |
| DLB-1300-8.0-P20 | 8 | 42 | 20 | 39 | 37.5 | - | 8 | 8 | 9.3 |
| DLB-1300-11-P20 | 11 | 42 | 28 | 37 | 37.5 | - | 10 | 9 | 6.9 |
| DLB-1300-11-P40 | 11 | 42 | 28 | 37 | 37.5 | 10.2 | 12 | 11 | 6.7 |
| DLB-1300-15-P20 | 15 | 42 | 30 | 45 | 37.5 | - | 12 | 11 | 5.2 |
| DLB-1300-15-P40 | 15 | 42 | 30 | 45 | 37.5 | 20.3 | 13 | 12 | 5.0 |
| DLB-1300-22-P20 | 22 | 57 | 30 | 45 | 52.5 | - | 12 | 11 | 6.8 |
| DLB-1300-22-P40 | 22 | 57 | 30 | 45 | 52.5 | 20.3 | 14 | 13 | 6.6 |
| DLB-1300-28-P20 | 28 | 57 | 35 | 50 | 52.5 | - | 14 | 13 | 5.5 |
| DLB-1300-28-P40 | 28 | 57 | 35 | 50 | 52.5 | 20.3 | 16 | 14 | 5.3 |
| DLB-1300-37-P20 | 37 | 57 | 42 | 56 | 52.5 | - | 14 | 14 | 4.2 |
| DLB-1300-37-P40 | 37 | 57 | 42 | 56 | 52.5 | 20.3 | 18 | 16 | 4.0 |